## Slide 1
Estimation of Residual Stress Distribution in MIG-Based WAAM Wall Structures Using FEM with an AI-Surrogate Model
Project presentation for mid semester evaluation on
Presented by Ashish Chaudhary
Entry No. 2025mem1022
Supervised by Dr. Ravi Kant
Department of Mechanical Engineering
Indian Institute of Technology Ropar, Punjab
22 September 2026

## Slide 2
01 — INTRODUCTION
Research Background & Motivation
Wire Arc Additive Manufacturing (WAAM) builds near-net-shape metal parts by depositing weld beads layer-by-layer, offering high deposition rates (1–9 kg/h) and low equipment cost relative to powder-bed AM.
MIG based WAAM is attractive for large metallic structures due to its high deposition rate and comparatively low heat input among arc processes.
Layer deposition causes repeated reheating and remelting, while wall dimensions and interlayer dwell time control heat dissipation and thermal accumulation.
Repeated heating/cooling causes non-uniform thermal expansion and contraction, driving distortion and residual stress in the build.
MIG-WAAM
High heat input
Repeated thermal cycles
Non-uniform heating / cooling
Thermal expansion & contraction
Residual stress + distortion
2

## Slide 3
01 — INTRODUCTION
Why Residual Stress Is a Critical Problem
Residual stress: internal stress that remains in a part after the external heat source and mechanical constraints are removed.
In layer-by-layer WAAM, residual stress originates from steep temperature gradients between the molten pool and the surrounding solid, combined with constrained thermal expansion/contraction on cooling.
Governs dimensional stability, distortion, and fatigue/structural performance of the built part.
Because it cannot be measured in advance, residual stress must be predicted before WAAM process parameters can be reliably optimised.
Conceptual origin of residual stress
Heat source (arc)
↓
Molten pool formation and Thermal Expansion
↓
Cooling & solidification
↓
Thermal contraction
↓
Constrained by solid base
↓
Residual stress
3

## Slide 4
S. No. | Author(s) / Year | Material | Methodology | Results / Key findings | Research Gaps / Limitations
1 | Schauenberg et al. (2024) | Base metal: ASTM A36 mild steel plate, 350×150×6.3 mm (GMAW T-joint, not a WAAM wall) | ABAQUS FEM: Goldak heat flux (GHF) via DFLUX subroutine at 3 different starting points , prescribed weld temperature (PWT) via element birth/death Combined GHF+PWT hybrid model proposed Validation via 4 K-type thermocouples | GHF_P1/P2 average error 4.14%/3.64% vs. thermocouples but poor prediction of fusion-zone shape and longest computation time PWT alone: 30.46% peak-temperature error, Combined GHF+PWT model: improved fusion-zone/HAZ correlation using only 15.04% of GHF_P1's computation time | [Author-stated] Neither Goldak nor PWT alone was fully satisfactory — motivated the hybrid model [Inferred] T-joint GMAW weld, not a multilayer WAAM wall , no residual stress reported [Inferred] No AI/ML
2 | Gupta & Mulik (2024) | Wire: mild steel filler Substrate: mild steel plate, 120×80×8 mm; 4 layers × 2 mm | ANSYS transient thermal FEA; Goldak double-ellipsoid heat source (Q=1800 W, η=0.83) 4 K-type thermocouples at 0, 6, 12, 18 mm from bead centreline | Max. temperature 2125.8 ℉ at Layer-3, dropping to 2035.6 ℉ at Layer-4 (radiative loss) Peak-to-peak relative error 13.77% at point E, reducing to 4.76% by 4th peak | [Author-stated] Idealised assumptions: constant torch speed [Inferred] Only temperature — residual stress not computed despite thermo-mechanical module available [Inferred] Mild steel only; Inconel not investigated; no AI/ML
3 | Gogulraj & Rajamurugan (2026) | Wire: IN-625 (Inconel-625) Substrate: mild steel CMT-WAAM single-pass beads | CMT-based WAAM; RSM + ANN optimisation of wire feed rate & travel speed Bead width, height, dilution measured; Optical microscopy, XRD phase analysis Residual stress via portable X-ray diffractometer (surface, near-bead) | ANN (R² = 0.9574 for bead height) RSM(R² = 0.9969 for bead height IN-625 – WFR 6200 mm/min → 4.95% dilution, 4.98×6.31 mm bead Residual stress (compressive)IN-625 −392 Mpa | [Author-stated] Only single-pass bead-on-plate geometry; not a full wall structure [Inferred] Residual stress measured only at the surface by XRD — no destructive (hole-drilling/contour) cross-check [Inferred] ANN used for bead geometry only, not integrated with a physics-based FEM thermal model (no FEM+AI surrogate)
02 — LITERATURE REVIEW
4

## Slide 5
Literature Synthesis: What Has Been Achieved?
1
WAAM PROCESS
Process parameters (current, travel speed, wire feed rate,voltage) strongly influence thermal history and bead geometry.
[Lambiase 2022; Pereira 2024]
2
FEM
Goldak-type heat sources reliably predict temperature fields and can be extended toward thermo-mechanical behaviour.
[Cadiou 2020; Schauenberg 2024; Gupta & Mulik 2025]
3
MICROSTRUCTURE / HARDNESS
Thermal cycling control grain morphology and hardness; act as an effective thermal-control parameter.
[Cheepu & Kantumuchu 2023; Chukenova 2026]
4
AI / DATA-DRIVEN
Residual-stress prediction not yet addressed.
FEM
Physics + Accuracy — but computationally expensive
AI
Speed + Fast prediction — but dependent on the quality/coverage of the training dataset
This complementary trade-off motivates a hybrid FEM–AI approach.
5

## Slide 6
03 — RESEARCH GAP
Identified Research Gap
EXISTING RESEARCH
FEM-based WAAM thermal modelling [Cadiou 2020; Gupta & Mulik 2025]
Goldak / hybrid heat-source implementations [Schauenberg 2024]
Heat-input → microstructure → hardness relationships [Cheepu & Kantumuchu 2023; Chukenova 2026]
LIMITATIONS
High computational cost of repeated FEM simulation
AI/data-driven work targets geometry & hardness
No FEM–AI integration for prediction of residual stress found in reviewed literature
CENTRAL RESEARCH GAP (as identified from the reviewed literature)
“There is a need for a validated hybrid FEM–AI framework that retains the physics-based capability of FEM while providing rapid residual-stress prediction for MIG-based WAAM wall structure.”
6

## Slide 7
03 — RESEARCH GAP
Problem Statement
Residual stress in MIG-based WAAM is governed by complex, nonlinear thermal and mechanical interactions. Although FEM can provide physics-based predictions, repeated high-fidelity simulations are computationally expensive. Conversely, AI models offer rapid predictions but may lack physics-based generalisation.
Therefore, a hybrid FEM–AI surrogate framework is proposed to achieve both predictive accuracy and computational efficiency for residual-stress prediction in WAAM wall structure.
High-fidelity FEM
Accurate but expensive
+
AI
Fast but data-dependent
↓
HYBRID FEM–AI
Physics + Speed + Accuracy
7

## Slide 8
04 — PROPOSED WORK
Research Objectives
1
1.Develop a transient thermo-mechanical FEM model of MIG-based WAAM Inconel wall structures.
2
2.Implement and calibrate a moving heat-source (e.g. Goldak double-ellipsoidal model) using process parameters and experimental data.
3
3.Predict temperature history and residual-stress distribution under selected WAAM process conditions.
4
5
5.Generate a reliable FEM dataset and develop an AI/ML surrogate model for rapid residual-stress prediction.
4.Experimentally validate the predicted residual stresses using an appropriate destructive or non-destructive measurement technique.
8

## Slide 9
04 — PROPOSED WORK
Proposed Hybrid FEM–AI Methodology
WAAM process parameters
(current, travel speed, wire feed rate,voltage)
↓
Thermal FEM — moving heat source / Goldak model
↓
Temperature history
↓
Mechanical FEM
↓
Residual-stress distribution
FEM dataset generation & pre-processing
↓
AI / ML surrogate model — training, validation, testing
↓
Rapid residual-stress prediction
↓
Experimental validation
↓
Model correction / final validation
Physics-based FEM stage
AI surrogate stage
9

## Slide 10
Timeline Task | Third Mid Semester |  | Third End Semester |  | Fourth Mid Semester |  | Fourth Semester |  | Fourth Semester | 
 | July 2026 - September 2026 |  | September 2026 - November 2026 |  | December 2026 – January 2027 |  | January 2027 - March 2027 |  | March 2027 - June 2027 | 
Literature review |  |  |  |  |  |  |  |  |  | 
FEM Thermal Model |  |  |  |  |  |  |  |  |  | 
FEM Thermo-Mechanical |  |  |  |  |  |  |  |  |  | 
Experiment and Residual-Stress measurement |  |  |  |  |  |  |  |  |  | 
FEM Validation/Callibration |  |  |  |  |  |  |  |  |  | 
AI Surogate Model Development |  |  |  |  |  |  |  |  |  | 
Hybrid model Validation |  |  |  |  |  |  |  |  |  | 
Final Analysis and thesis/Publication |  |  |  |  |  |  |  |  |  | 
Completed
In Progress
Future Plan
5 - Proposed Work Plan
10

## Slide 11
6 - Conclusion
1. WAAM thermal cycling and heat accumulation significantly influence residual stress and distortion.
2. FEM provides physics-based residual-stress prediction but is computationally expensive.
3. AI surrogate models can enable rapid prediction but require reliable FEM-generated datasets.
4. A research gap exists in FEM–AI integration for residual-stress prediction in MIG-WAAM Wall structure.
11

## Slide 12
REFERENCES
Key Literature Cited
Cadiou, S., Courtois, M., Carin, M., Berckmans, W., Le Masson, P. (2020). 3D heat transfer, fluid flow and electromagnetic model for cold metal transfer wire arc additive manufacturing (CMT-WAAM). Additive Manufacturing, 36, 101541.
Schauenberg, A.S., Rodríguez, R.Q., Almeida, D.T., Zanon, J.E., Cunha, E., Lopes, A.P.O., Tonatto, M.L.P. (2024). Evaluating thermal gradient in GMAW welding process with a novel heat source model: numerical and experimental approach. Engineering Structures, 318, 118724.
Lambiase, F., Scipioni, S.I., Paoletti, A. (2022). Accurate prediction of the bead geometry in wire arc additive manufacturing process. International Journal of Advanced Manufacturing Technology, 119, 7629–7639.
Pereira, A.S., Costenaro, F., Gonçalves e Silva, R.H., Marques, C. (2024). Control strategy for geometry at the start and end of bead in WAAM steel walls using a custom GMAW DF power source (MIG-AD). International Journal of Advanced Manufacturing Technology, 135, 5341–5352.
Chukenova, E., Nugman, E., Kanagat, B., Kentaikyzy, B.A., Mustafa, A., Alexander, K., Jaskari, M., Jarvenpaa, A., Khatir, O., Hamada, A.S. (2026). Optimization of electric arc parameters for structural changes in parts obtained using WAAM technology. International Journal of Advanced Manufacturing Technology, 145, 3405–3415.
Cheepu, M., Kantumuchu, V.C. (2023). Numerical simulations of the effect of heat input on microstructural growth for MIG-based wire arc additive manufacturing of Inconel 718. Transactions of the Indian Institute of Metals, 76(2), 473–481.
Gupta, D.K., Mulik, R.S. (2025). Numerical simulation and experimental investigation of temperature distribution during the wire arc additive manufacturing (WAAM) process. Progress in Additive Manufacturing, 10, 631–645.
12

## Slide 13
THANK YOU
13